## Slide 1: Wide Angle Scattering and Pair Distribution Functions
Dr Katharina Edkins
The University of Manchester
@k_edkins

## Slide 2: Overview
Diffraction
  What are the effects of increasing disorder?
Small vs wide angle scattering
Pair distribution function
Examples

## Slide 3: Diffraction

## Slide 4: Diffraction
Birkbeck College

## Slide 5: The effect of temperature
T = 0K
T > 0K

## Slide 6: The effect of dislocation
Single-crystal diffuse scattering studies on polymorphs of molecular crystals. I. The room-temperature polymorphs of the drug benzocaine.
E.J. Chan, T.R. Welberry, D.J. Goossens, A.P. Heerdegen, A. Beasley, P.J. Chupas
DOI:10.1107/S0108768109015857

## Slide 7: Nanoscale structure
Science, 2007, 316, 561

## Slide 8: Wide vs small angle scattering
Wide Angle Scattering < 10-9 m
Small Angle Scattering > 10-9 m

## Slide 9: Wide vs small angle scattering
Polym. Chem.,2016, 7, 5004–5010
4˚ 2θ
Amorphous poly(phosphoamidate), data acquired with Cu Kα radiation (λ = 1.54 Å)
40˚ 2θ: d = 2.25 Å
30˚ 2θ: q = 2.1 Å-1
2.7 nm

## Slide 10: Pair distribution function
© Alan Soper

## Slide 11: Pair distribution function
© Alan Soper

## Slide 12: Pair distribution function
© Alan Soper

## Slide 13: Pair distribution function
© Alan Soper

## Slide 14: Pair distribution function

## Slide 15: Pair distribution function

## Slide 16: Pair distribution function
Measurement in reciprocal space gives structure factor F(q)
F(q) and S(q) are related to respective g(r) by Fourier Transform
Partial structure factor

## Slide 17: Indomethacin in polymer
V. Petkov, Y. Ren, S. Kabekkodu, D. Murphy, Phys. Chem. Chem. Phys., 2013, 15, 8544

## Slide 18: Silver nanoparticles in zeolite
D. O’Nolan, H. Zhao, Z. Chen et al., Chem. Sci., 2021, 12, 13836

## Slide 19: Structure solution from WAXS
Problem: fitting of too many parameters to one structure factor!
D. Prill, P. Juhas, M.U. Schmidt, S.J.K. Billinge, J. Appl. Cryst., 2015, 48, 171

## Slide 20: Wide-angle neutron scattering
H/D
H/H
D/H
D/D

## Slide 21: WANS
i | j | ci | cj | bi, fm | bj, fm | cicjbibj = wij, fm
O | O | 1/3 | 1/3 | 0.5804 | 0.5804 | 0.0374
O | H | 1/3 | 2/3 | 0.5804 | -0.3741 | -0.0482
H | H | 2/3 | 2/3 | -0.3741 | -0.3741 | 0.0622
Water
i | j | ci | cj | bi, fm | bj, fm | cicjbibj = wij, fm
O | O | 1/3 | 1/3 | 0.5804 | 0.5804 | 0.0374
O | D | 1/3 | 2/3 | 0.5804 | 0.6674 | 0.0861
D | D | 2/3 | 2/3 | 0.6674 | 0.6674 | 0.1980
Heavy water

## Slide 22: WANS

## Slide 23: WANS
Each isotopic mixture gives one structure factor
Different correlations can be extracted from each structure factor
https://www.isis.stfc.ac.uk/OtherFiles/Disordered%20Materials/DM%20Isotopic%20Substitution%20Experiments%20v1.0.pdf

## Slide 24: Generation of structural models
EPSR (empirical potential structure refinement)

## Slide 25: Generation of structural models
N.H. Rhys, A.K. Soper, L. Dougan, J. Phys. Chem. B, 2012, 116, 13308

## Slide 26: Applications

## Slide 27: Water
A. Soper, C.J. Benmore, Phys. Rev. Lett., 101, 065502

## Slide 28: Antifreeze effect
J.J. Towey, A.K. Soper, L. Dougan, Faraday Disc. 2013, DOI 10.1039/c3fd00084b

## Slide 29: Small peptides
S. Busch, C.D. Bruce, C. Redfield, C.D. Lorenz, S.E. McLain, Angew. Chem. Int. Ed., 2013, 52, 1

## Slide 30: Drug compounds
L. Tavagnacco, J.W. Brady, F. Bruni, S. Callear, M.A. Ricci, M.L. Saboungi, A. Cesaro, J. Phys Chem. B, 2015, 119, 13294

## Slide 31: Ionic liquid/ salt melt
C. Hardacre, J.D. Holbrey, S.E.J. McMath, D.T. Bowron, A.K. Soper, J. Chem. Phys., 2003, 118, 273
Imidazole-chloride distance
Imidazole-imidazole distance

## Slide 32: Heterogeneous catalysis
T.G.A. Youngs, H. Manyar, D.T. Bowron, L.F. Gladden, C. Hardacre, Chem. Sci., 2013, 4, 3484

## Slide 33: Conclusion
Wide angle scattering gives atomic resolution data
Potential samples are
  disordered crystalline materials
  Nanomaterials
  Solutions
  Glasses
Using WANS and WAXS in combination with Monte Carlo simulation can give a structural snap-shot of the disordered phase