## Slide 1: Chemical Applications of Neutron Scattering: ISIS Neutron School 2022
Stuart Clarke
BP Institute, Department of Chemistry,
University of Cambridge, UK
Lots of examples centred on ‘adsorbed Layers’

## Slide 2: Talk Outline
Neutron scattering
      Coherent scattering - structure
      Incoherent scattering - dynamics
Examples of surfaces / neutron applications:
We use LOTS of different techniques to answer complex problems
Too much to cover…. See how far we get..
Adsorbed layers:
In-plane structure – 2D diffraction (D20)
Out-of-plane structure – reflection (SURF, CRISP, INTER, POLREF, OFFSPEC)
What’s adsorbed? (IQNS - dynamics) IRIS
Colloidal dispersions (dominated by surfaces)
What’s on the surface? SANS (LOQ)
What arrangement ? SE- SANS
Liquid structure PDF (SANDALS, NIMROD)
Conclusions
Notes: Mid ground between materials chemistry, physical theory, physical characterisation, engineering etc..

## Slide 3: Conclusions
Neutrons
Very powerful tool(s) for Structure (Dynamics)
Contrast between H and D very useful: highlight
Can ‘see’ Hydrogen: Highlight
- Excellent transmission (extreme/commerical conditions)
BUT.
- Tricky to get hold of/limited access
(complement with other methods)
Notes: Mid ground between materials chemistry, physical theory, physical characterisation, engineering etc..

## Slide 4
Examples of Monolayers
Wetting
Colloidal Stabilisation
Detergency
Lubrication
Academic and industrial issues:
Colloidal stablisation, molecular patterning,
wetting behaviour, detergency,
Slip agents, liquid crystals.
Corrosion,
Solid monolayers
‘Buried’ monolayers
inaccessible to study:
Need to get through bulk phase
-neutrons have great transmission
Unusual experimental approaches
Mixtures / Multicomponent:
Cheaper …
Notes: Adsorption to solid
PAUSE!!
Adsorbed layers central to many phenomena:
Motivation.
Dyes used to enhavnce spectral range of PV’s, patterning
Adsorbed surfacts for coloidal stability
Detergency synergy multicomponent mixture
In many cases ordered layers crucial:
Boundary lubrication
wetting behaviour:condensing vapour onto surface
Orderd layers can inhibit complete wetting
structual missmatch.
Particularly solid monolayers!!!
Other places interfaces crucial: Types of wetting-I, II, III?
Even strongly attractive surfaces can show
incomplete wetting due to formation of
solid/crystalline layers-lattice mismatch
Ordered layers very important in boundary lubrication.
Liquid crystal alignment etc.
Advanced from mere speculation about the existence of solid monolayers to subtle details of crystal packing.

## Slide 5: Talk Outline
Examples of surfaces / neutron applications:
Adsorbed layers:
In-plane structure – 2D diffraction
Out-of-plane structure – reflection
What’s adsorbed? (IQNS - dynamics)
Colloidal dispersions (dominated by surfaces)
What’s on the surface? SANS
What arrangement ? SE- SANS
Liquid structure PDF (NIMROD)
Notes: Mid ground between materials chemistry, physical theory, physical characterisation, engineering etc..

## Slide 6: 3D diffraction: crystallography
‘Work horse’ of chemical community
Crystal structures of minerals, materials, organic molecular structure determination.
Neutrons very good at hydrogen (x-rays no so good)
Adjacent elements (look the same to x-rays)
TODAY: 3D  2D diffraction

## Slide 7
Less
Equals
In-plane 2D Structure:
X-ray and Neutron diffraction
Neutrons: sensitive to hydrogen
X-rays: greater precision
Independent information
Combination is often essential
Decane on graphite
Octane on graphite

## Slide 8
Why Xrays AND neutrons are important.

## Slide 9: Chloromethane monolayer: X-rays
Morishige, et al., Mol Phys , 72 395-411 (1991). 'The Structure of Chloromethane Monolayers Adsorbed on Graphite'.
X-ray
Low coverage
Chlorine atoms
Where are CH3 groups?
Guessed:
Ferro electric ordering?
Like bulk crystal plane…
Bulk Plane

## Slide 10: Chloromethane
Morishige, et al., Mol Phys , 72 395-411 (1991). 'The Structure of Chloromethane Monolayers Adsorbed on Graphite'.
Neutron
X-ray
Monolayer
Low coverage
Need neutrons to see CH3 groups and full symmetry
Bulk Plane
With neutrons:
Anti ferroelectric
Alternating chains

## Slide 11: Mixing: How do you tell if two species like each other?
1) They avoid each other  phase separation:

## Slide 12: Mixing ideally

## Slide 13: Special relationship; stoichiometric complex Molecular compound

## Slide 14
Structure: Diffraction from Mixed Monolayers
How do molecules mix on a surface?
(a) Phase sep. (b) Mixing (c) Molecular compound
Pure A
Molecular Compound
Pure B
Pure B
Pure A
Hexanol/heptanol
Heptanol/octanol
Heptanol/nonanol
Composition 
Angle 
Intensity 
Pure C7OH
Pure C9OH

## Slide 15
‘Special, non-covalent bonding between molecules’
Big topic of supramolecular self assembly
Donation of lone pair from nitrogen to Iodine ataom

## Slide 16: Novel Chemical interactions: Halogen Bonded co-crystal
Monolayer
N….I-C
‘New hydrogen bonds’
Very stable layers
2DT>> 3DT
Directional
Strong
‘Controls’ strength
and orientation

## Slide 17: 2D –diffraction: summary
Can see in-plane molecular structure.
(non-invasive)
X - ray and neutrons can be essential : Neutrons ‘see’ H
Determine surface phase behaviour
Characterise inter molecular bonding

## Slide 18: Talk Outline
Examples of surfaces / neutron applications:
Adsorbed layers:
In-plane structure – 2D diffraction
Out-of-plane structure – reflection
What’s adsorbed? (IQNS - dynamics)
Colloidal dispersions (dominated by surfaces)
What’s on the surface? SANS
What arrangement ? SE- SANS
Liquid structure PDF (NIMROD)
Notes: Mid ground between materials chemistry, physical theory, physical characterisation, engineering etc..

## Slide 19: Neutron Reflection: how does it work?
Reflection of neutrons from the
solid/liquid interface at grazing
angles
  Collect reflected intensity as a function of ‘angle’ (q)..
  Solid substrates and coated surfaces
Extend to new solid/liquid Interfaces: iron oxides, stainless, alumina, Ti oxides, Ni, Cu …
(previously: silica, Al2O3)
New conditions:
applied shear

## Slide 20: Neutron Reflection Theory
Chart: q, Å-1

## Slide 21: Neutron Reflection Theory
Chart: q, Å-1

## Slide 22: Neutron Reflection Theory
Chart: q, Å-1

## Slide 23: Neutron Reflection Theory
Chart: q, Å-1
Film thickness
Layer thickness
Substrate
Liquid
‘Fit’ experimental data to model.
 How much material at the surface
Layer ‘structure’
Non-invasive/in-situ
Position of critical edge key indicator of solution composition
(Tutorial problem)
BIO:
Supported bilayers key theme of recent bio- studies
Representing biomembranes…
(with proteins etc.)

## Slide 24: Thin layer reflection: Add amplitudes
Tutorial problem: geometric series

## Slide 25: Neutron: ‘Magic’
Contrast matching..
Making things disappear!
Unique structural solution.
 BIG advantage of neutrons
Need to make sure complete exchange of solutions.. Not always easy..
Ask me about ‘baby oil’?
BUT: bio-molecules very complicated/hard to prepare.
(dedicated facilities at some Institutes)

## Slide 26: Reflection Example #1
Calcite (CaCO3)
Very important mineral
Scale in your kettle
Oil reservoirs
Overbasing agent in engines
What adsorbs and how?
In oil? In water?
Polymers? Surfactants?
(Birefringent…! Double refraction)

## Slide 27: Neutron reflection: Example #1 Surfactant, AOT, on Calcite (CaCO3) in oil
Chart: q, Å-1




Adsorption of a monolayer on a surface:
(The bare surface, monolayer and bilayer calculations)
Why a monolayer adsorb in oil and not a bilayer?
What adsorbs in water…..?

## Slide 28: Reflection Example : Additives on calcite..
Monolayers, Bilayers,
multilayers and adsorbed polymers
Surface corrosion
Molecular precision!
Notes: Mention other interesting challenges we can address: fatty acids, more detailed AOT from oil, asphaltenes and resins; also other mineral surfaces: Si in progress, any other one where we get good crystals

## Slide 29: (Kate Miller) Layered silicate: mineral books
Mica:
Clays are key component of many oil reserviors
Very common in AFM/SFA studies
Many attempts to study with neutron reflection failed
To hard to get a beam through
Can’t deposit through vapour
Thin sheets too flexible/break.. So..?
Reflection Example : Mineral Surfaces - mica

## Slide 30: ‘Peeling’ Mica
silicon
‘Glue’
Mica
Support very thin layers on solid substrate and ‘peel’
Does it work?.......
Can we see adsorption on mica in solution?…

## Slide 31: Surfactant adsorption on mica
Non-invasive:
(a) DiDoDAB: Complete bilayer
(same result as AFM)
(b) CTAB: NOT same as AFM
AFM
Mica
Surfactant bilayer
Neutrons
Neutrons non-invasive
Rather thick layers of glue and Mica – does this change the reflection?
(‘Advanced’ tutorial problem)

## Slide 32: Example: Layers under Shear
Do layers get swept off under shear?
(steady and oscillatory shear)
Modest shear rates < 500s-1
(pipe flow, or flow over rock-beds)

## Slide 33
Thin layers
Thick layers
Shear/Flow:
AOT on Alumina/water

## Slide 34
Very thin layer - too thin for significant shear effects.
(Same result under oscillatory shear).
Neutron reflection data: D17
SURFACTANT BILAYER (thin layer approx. 30A thick)
Data: under steady shear increasing to approx 1000s-1:
Effects of Shear: neutron reflection:
Thin layer
Shear has no effect
on thin layer

## Slide 35
Adsorbed multi layer
Thick layer!!
Under steady and oscillatory shear:  BIG effects
Critical shear rate that delaminate the layers
Effects of Shear: neutron reflection:
Thick layer
Higher shear rates planned
Shear has big effect
on thick layers

## Slide 36: Talk Outline
Examples of surfaces / neutron applications:
Adsorbed layers:
In-plane structure – 2D diffraction
Out-of-plane structure – reflection
What’s adsorbed? (IQNS - dynamics)
Colloidal dispersions (dominated by surfaces)
What’s on the surface? SANS
What arrangement ? SE- SANS
Liquid structure PDF (NIMROD)
Notes: Mid ground between materials chemistry, physical theory, physical characterisation, engineering etc..

## Slide 37: Quasi-elastic neutron scattering
Diffusive motions
How long to move out of your ‘box’

## Slide 38: Incoherent Neutron Scattering
Actually get a distribution of scattered neutron energies:
DE
Intensity
Details of the angular dependence of the scattering can inform us about molecular motions
Very high energy resolution, 1 meV
IN10/IN16/IRIS

## Slide 39: Hydrogen and Deuterium are different
Hydrogen – very strong scatterer
Deuterium – weak scatterer
In a mixture can use neutrons to choose what we ‘see’

## Slide 40: Quasi-elastic Incoherent Neutron Scattering (IQNS) – ‘Dynamics’
Neutrons can exchange energy with sample nuclei:
Translating nuclei
Slowed down
Speeded up
‘Inelastic’
Liquids
Isotopic substitution to distinguish components (H>>D)
Dynamics to differentiate adsorbed from non-adsorbed materials
‘Elastic’
Static
Solids
Sample
Intensity of elastic scattering  Amount of adsorbed, ‘NOT-MOVING’ material

## Slide 41: Adsorbed Molecules are different
surface
Adsorbed layers are ‘static’
Liquids are ‘dynamic’
Use mobility to distinguish adsorbed layers
Monolayer
(solid)
Bulk
(liquid)

## Slide 42: ‘IQNS’ What’s adsorbed?
Component of interest (protonated)
Other component(s) (deuterated)
Only ‘see’ protonated bits
Bulk
(liquid)
Monolayer
(solid)
‘Elastic’ scattering
Only ‘see’ contribution from component of interest in the monolayer
surface

## Slide 43: Incoherent quasi-elastic neutron scattering (IQNS)
What do we expect to see if there is a solid
monolayer coexisting with the bulk liquid?

## Slide 44
IQNS Results: Octane on Graphite
Bulk melting point
Monolayer Level
Monolayer melting point
How much is in this monolayer?
(Tutorial Problem)

## Slide 45
What’s adsorbed: (IQNS) Results from mixtures
Octane/nonane
Octane/decane
Monolayer composition as a
function of solution composition
Plateau level falls as octane
is displaced by decane

## Slide 46: Dynamics of Adsorbed Layers
Distinguish solid from liquid
  elastic scattering
Diffusion coefficient of liquid layers
  Width of the quasi-elastic peak
Rotation of molecules
  q-dependence of the elastic scattering
Mark Johnson

## Slide 47: Talk Outline
Examples of surfaces / neutron applications:
Adsorbed layers:
In-plane structure – 2D diffraction
Out-of-plane structure – reflection
What’s adsorbed? (IQNS - dynamics)
Colloidal dispersions (dominated by surfaces)
What’s on the surface? SANS
What arrangement ? SE- SANS
Liquid structure PDF (NIMROD)
Notes: Mid ground between materials chemistry, physical theory, physical characterisation, engineering etc..

## Slide 48: What are Colloids?
Tiny objects (10 nm – 10 mm)
Dispersed in a continuous phase
Plates
Examples (lots…) Fog – water droplets in air
  Blood – particles in ‘water’
  Milk – liquid fat drops in water (emulsion)
  Foam – air bubbles in a liquid or solid
  Important flow properties
  Need to ‘look’ through metal cells
  Opaque samples
  Neutron Transmission
Spheres
‘nanoparticles’
Want to know
What shape are the separate colloids
What orientation
What arrangement
Soft-matter: SANS a key approach:
Characterisation of polymers/emulsions/gels

## Slide 49: Form and Structure Factors
S(q)
I(q)
P(q)
q
Dilute Spheres
Crystal
Liquid
Characterise particles
Diffraction peaks
‘Liquid’ ring
I(q)
S(q)
I(q)
P(q)
S(q)
I(Q)=P(Q)S(Q)
P(q)
P(q)
I(q)

## Slide 50: SANS: single colloid scattering (Dilute) What’s on the surface

## Slide 51: Mixtures: Contrast matching: ‘magic’
Scattering from silica in water: Mixtures of H2O and D2O
Change scattering of water
(refractive index = ‘colour’):
silica –disappears
‘See’ each component of a mixture separately
Simplify complex systems

## Slide 52
P(Q) form factor for core-shell more complex
Structure: core/water/surfactant/oil
Small Angle Scattering: - P(Q)
Dilute core-shell particles
Thin water layer on calcite colloids in oil
‘Contrast variation’
H2O and D2O mixtures
change ‘colour’ of different bits
26.3 Ǻ
CaCO3
H2O
D/H-cyclohexane
Surfactant sheath
2.7 Ǻ
8.8 Ǻ
Thanks to Richard Heenen and co

## Slide 53: Contrast variation:
Enhance sensitivity to each bit by selective deuteration

## Slide 54: IF TIME SANS: Single particle orientation
SANS of plate-like particles

## Slide 55
Flow
Direction
Anisotropic Particles
When is the extent of orientational order?
Under flow?
With particle size?
Aspect ratio?
Concentration?
Use crystalline nature of particles to obtain full three-dimensional orientational distribution function
Completely random particle distribution => ‘powder’ ring
Perfectly aligned => single ‘spot’
Preferred orientation => ‘arc’ of intensity
SANS: single particles - orientation

## Slide 56
Measuring orientational order of plates
Only crystals in the correct orientation will diffract
Intensity gives number of crystals at each orientation in a sample
Steady Flow
Orientational order of the plates in flow

## Slide 57
Dense Clay pastes under static and cross-flow conditions

## Slide 58: Two colour cars

## Slide 59: END of EXTRA BIT

## Slide 60: SANS: Interference Between Objects
Consider scattering as distribution of spheres
  Isolated object, e.g. spheres (P(Q))
  S(Q) is called the interference or ‘structure factor’: interference from different colloids.
  Measured intensity is:
  I(Q)=P(Q) x S(Q)
Other systems:
  Crystal - unit cells repeat on a regular lattice
Eg Colloidal dispersion

## Slide 61: Colloidal crystals of spheres
Diffract light … Gives ‘diffraction patterns’
 Use diffraction to give structure

## Slide 62
Colloidal Spheres under flow
Crystal
Perfectly ordered sequence
of perfect hexagonally ordered layers
‘Layers’
Perfect hexagonally ordered layers
Sliding over each other with many different positions
‘Strings’
Particles in lines
A
C
B
Flow
Gradient
Increasing Shear Rate
‘Crystal’
‘Strings’
Charged stabilised
latex spheres 8%
‘Sliding layers’
Behaviour like ‘atoms’ only much larger scales and slower

## Slide 63
Single Layer
Stacked Layers
‘Real’ Space
‘Scattering’ Space
Structure in the stacking sequence reflected in intensity variations along ‘Bragg rods’  3D FCC
S(Q): Scattering Patterns from Layered Systems

## Slide 64
IF – TIME
EXTRA BIT SE- SANS
TRICKY!!!!

## Slide 65
SANS  SE-SANS VERY BIG objects
Big objects are seen at small scattering angles (‘Reciprocal space’)
To see scattering by SANS at small angles need VERY tightly collimated beam: BUT THEN NO FLUX!!
Spin echo SANS  Keep wide open beam and
Encode the scattering angle in the neutron spin!!
(VERY CLEVER IDEA THIS!!)

## Slide 66: Spin Echo -SANS Encode scattering angle in the neutron polarisation
Sample
Precesses in magnetic field
‘Un-winds’ in magnetic field
Gives an ‘echo’
Polarised neutron beam
Andersson 2008
Anisotropic magnetic fields
Collect intensity as a function of ‘z’ (combination of field angle, wavelength etc)
(Precession usually in horizontal plane)

## Slide 67: SE SANS technique: Basic approach
Beam polarised in and out
Polarisation rotates one way and then back
Depends upon time in the magnetic fields
If neutrons don’t change direction  big echo
If neutrons change direction (funny shaped field)  Weaker ‘echo’ or depolarised.
Spin echo to encodes the angle ( q’)
 Actually Measure:
Real space, density-density correlation function, G(z)

## Slide 68: Example: Silica particles in polymer matrix Colloidal Crystal
J. Baumberg Samples:
Hexagonal layers of 200nm silica in polymer matrix, 0.47 volume fraction.
Layers oriented and regularly stacked
Volume fraction 0.47 silica spheres
Ordered by ‘bending’ process
Stacked in layers.

## Slide 69
(iii) First correlation peak is less ordered than expected.
(iv) Higher order correlations of a true crystal are lost.
Clearly indicates significant positional disorder in the ‘crystal’.
‘Ordered’ array of spheres: SE-SANS
Core radius (big!): 90nm (good agreement)
Vol fract as z ∞, 0.22 in reasonable agreement.
Small z-sphere form
Long z- sphere packing fraction
Intermediate z- inter particle correlation
Larmor  NEW INSTRUMENT

## Slide 70: End SE-SANS extra bit

## Slide 71: Talk Outline
Examples of surfaces / neutron applications:
Adsorbed layers:
In-plane structure – 2D diffraction
Out-of-plane structure – reflection
What’s adsorbed? (IQNS - dynamics)
Colloidal dispersions (dominated by surfaces)
What’s on the surface? SANS
What arrangement ? SE- SANS
Liquid structure PDF (NIMROD)
Notes: Mid ground between materials chemistry, physical theory, physical characterisation, engineering etc..

## Slide 72: Can we ‘understand’ liquid structure?
No long range order: NO diffraction??
Oh dear!!
But still a lot of structure..

## Slide 73: Radial distribution function
Liquid species

## Slide 74: Radial distribution function
r
How many species in this shell at distance r from the central one: g(r)
Liquid species

## Slide 75: Pair distribution function: g(r) (normalised)
‘Hard’ core…
Nearest neighbour shells..
…

## Slide 76: Pair distribution function: g(r), FT of scattering data
Chart: Q /Å-1
Fourier Transform
Measured data (NIMROD)
g(r))

## Slide 77: Can we ‘understand’ liquid structure? See all Atom-Atom distances
Separate different atom contributions by isotopic exchange (H and D):
a) First difference (big circles exchanged):
b) Second difference:
 ONLY solute-solute distances!!

## Slide 78: PDF example: Acetonitrile
See correct molecular structure at short distances
Solvent shells at
Longer distances
Chart: r /Å
Chart: r /Å

## Slide 79: Supercapacitors: Ions in acetonitrile
TPA Br in acetonitrile:
See ‘ion pairs’
Br-

## Slide 80: Talk Outline
Neutron sources
      Coherent scattering - structure
      Incoherent scattering - dynamics
Examples of surfaces / neutron applications:
Adsorbed layers:
In-plane structure – 2D diffraction
Out-of-plane structure – reflection
What’s adsorbed? (IQNS - dynamics)
Colloidal dispersions (dominated by surfaces)
What’s on the surface? SANS
What arrangement ? SE- SANS
Liquid structure PDF (NIMROD)
Conclusions
Notes: Mid ground between materials chemistry, physical theory, physical characterisation, engineering etc..

## Slide 81: Thanks..
Adam Brewer Halogen bonding:
Kate Miller/Lucy Griffin/Seung Lee: Calcite and Mica
Beth Howe/ Becky Welbourne (Phoebe Allen): PDF
Tom Arnold (DIAMOND): Alkane diffraction

## Slide 82
ILL/ISIS / KEK/ LLB/ Berlin..etc.
– neutron Time
DIAMOND/SLS – SAXS time
All the (Long suffering) beamline scientists
Thank YOU !